Dental material

Sheet no. 10

Dental Ceramics

** In the previous lecture we classified dental ceramics based on the particle nature into :

- glassy ceramics ( pure glasses )

Ex. Feldspathic porcelain and Hot pressed Ceramics .

- particle filled ceramics ( glass particle ) “ crystalline form that contain glass )

Ex. Lithium disilicate commonly known as IPs E.max .

- polycrystalline ( densely sintered )

Ex. YTZP ( yttrium stabilized tetragonal polycrystals ) which commonly known as “ zirconia ceramics “

AND alumina polycrystals .

** now what is available and commonly used in our practice are :

- E.max  from particle filled ceramics .

- Zirconia  from polycrystalline

- Feldspathic  porcelain  from pure glasses .

we have been also talked about “ bilayered ceramics “  and “strengthening mechanism “ , which may be through adding a metal layer from below or from the prepared tooth structure such as in PFM crowns ( as we have took in the lab and we will see next year ) ,

Or through bonding with the tooth structure as we do with “ laminate veneers “ .

Or by using strong materials “ coping “ such as zirconia and lithium disilicate as core materials  .

currently we have what is so called “ Monolithic “ or “ monolayered “ ceramic materials , the purpose of them is to combine strength and beauty ( esthetic  ) at the same time .

** As we have talked in the previous lecture , when we increase the crystalline phase of the ceramics  our Crown will be more stronger , but more opaque “ which mean less esthetic “ , On the other hand , when we increase the glassy phase of the ceramics  Our Crown will be more esthetic , but will have less strength .

** Nowadays , we have what so called “ ice zirconia “ which have more esthetic and enough strength .

** also , lithium disilicate ceramics have a good esthetic and good strength at the same time that made them suitable to be used for construction a 3 units anterior bridge “ in the past , this was not applicable , they used the bilayered ceramics for the anterior area , however , nowadays we were able to do full contour ( monolayer ) zirconia or lithium disilicate crowns .

** we also talked about the fabrication of ceramics which is done by :

- sintering

- casting ( ceramming )

- pressing

- CAD / CAM machines or copy milling machines

Regarding Sintering :

It means Heat , and we put the porcelain powders and this powder is added to a binder which is Water OR some Fluid similar to water added to it some molecules , this water is made as slurry ( wetted and flowy  sand ) , and this slurry is manipulated by technician “ layer by layer “ , then it is put in the furnace and the temperature is adjusted according to the porcelain powder used ( High fusing porcelain , Medium fusing porcelain , Low fusing porcelain and Ultralow fusing porcelain ) .

** With metal , we use the Low fusing porcelain OR the Ultralow fusing porcelain ; because we don’t want to use high temperatures that will cause the metal to melt .

** Ultralow fusing porcelain is used with Titanium ; because titanium requires high casting temperatures .

** feldspathic porcelain is only manufactured by Sintering .

** feldspathic porcelain is considered a Veneering Ceramic , only applied on the “ outer layer “ of ceramics .

** As we know , we have been divided the ceramics according to the function into :

- Veneering ceramics

- Core ceramics

And feldspathic porcelain OR the pure glassy ceramics OR even lithium disilicate can be used as a veneering ceramics “ outer layer “ .

** thus when we have a challenge in selection ( shade matching ) . in central incisors we focus mainly on pure glassy ceramics of feldspathic porcelain .

** lithium disilicate is considered to have its own “ feldspathic porcelain “ .

** before , when the porcelain was used in houses ( not in dentistry ) it was composed of Kaolin , Quartz ( silica ) and feldspar . In these porcelain the kaolin was a major component about 70% ; but in dentistry , when we used feldspathic porcelain the main component , were feldspar and Quartz , and the percentage of kaolin does not exceed 3% .

** thus , the good properties of our dental porcelain are provided by Quartz ( silica ) and feldspar , which has a role in modifying the quartz ( network modification ) to the silica particles . Quartz is a very strong solid material and require very high amounts of heat to melt about 3000 C .

** feldspar is compose of sodium aluminosilicate OR potassium aluminosilicate .

** the dental feldspathic porcelain ( the dr. show a phase diagram ) , when we increase the temperature to 1000 C .

We are doing sintering , when we reach reach a central area ( shown in the diagram ) we will have a point between “ sintering “ and “ vitrification “.

Vitrification means that we have a crystalline matrix , as we increase the temperature we are moving into a crystalline phase . this is the last thing we want in porcelain .

Thus the porcelain furnaces that we use have a computer controlled temperature , because we don’t want the temperature to exceed a certain limit, if certain limit is exceeded ( over heating ) we will have a crystalline deposition which in turn will give a dull appearance to the feldspathic porcelain affecting the esthetic ( less esthetic ) , and this is known as ( devitrification ) .

** we have talked previously that if we want to increase the crystal deposition to increase the strength we have to raise the temperature , but slowly from 6 -8 hours , in this period the crystals are rearranged in a certain pattern that will allow the light to pass through it ( translucency that we desire ) with more strength .

** this was used in “ leucite based empress ceramics “ , The percentage of leucite used with the feldspathic porcelain that is used with the metal is about 20% .

As we know , if we want to increase the strength of a ceramics we add leucites .

** the leucite percentage is increased from 40 – 55 % if we want to strengthen our ceramics .

** In lithium disilicate the leucite particles are about 70% .

** failure of ceramics Vs. failure of metal :

- metal failure is indicated by metal deflection.

- Ceramics failure is indicated by crack .

*** Ceramic Repair Kit :

in the patient mouth we should have :

- sandblaster ( Air Abrasion ) .

- saline coupling agent OR metal alloy primer .

- hydrofluoric Acid itch  for the areas covered by porcelain .

- composite .

Its not an easy job to do .

Thus , before starting our work we should know the suitable materials to use ,

1. EX. For long span bridge I should use a certain type of metal while for a short span bridge I should use another type of metal .

2. When we have high shear stress such as in “ Maryland bridges “ , we require a very stiff type of metal to prevent metal deflection .

** when we have deflection , the metal will move , and the porcelain on the top may break and show metal underneath .

** feldspathic porcelain is done very well as inlays , onlay , then we incorporated the leucites , and as we know the leucites are control crystalline phase that causes “ dispersion strengthening “ it increase the strength of the ceramics .

** It was also discovered that the leucites have 2 additional features , so we have :

- dispersion strengthening , we have a crystal phase in the middle that prevents crack propagation when it is available in 17 – 20 % with feldspathic porcelain .

- the leucites are attacked by hydrofluoric acid itch faster than feldspathic porcelain , this will give micromechanical roughness , this micromechanical roughness give us a stronger bond strength with resin cement , that’s why one of the best ceramics for adhesive cementation are itchable  ceramics , ( ie. Leucite resin forced feldspathic porcelain ) .

we have 20% of leucite that will disappear after itching ( providing the micromechanical roughness leaving uniform spaces for the resin cement and provide a strong bond .

- the coefficient of thermal expansion of leucites is similar to the coefficient of thermal expansion of cast alloys we are using .

these features gave the leucite reinforced feldspathic porcelain to be the best type suitable for veneering of metals , Zirconia and even for lithium disilicate .

** we have said that when we use the leucites in a percentage of 17 – 20% it reinforces the feldspathic porcelain by dispersion strengthening . If the percentage of leucite is increased to 45 – 55% this will provide more strength by one and a half folds than normal “ leucite reinforced feldspathic porcelain “ , this is used in “ cerraming “ technique , ( Remember , 2nd method of ceramics fabrication ) , and it uses heating in a controlled way for more than 8 hours ( EX. Pyrex ) .

** In Hot Pressed ceramics , the percent of leucite is 40 – 55%.

** OR we can use lithium disilicate or lithium orthophosphate m which is 3 times stronger , that’s why we are no longer using IPS empress 1 , we use IPS empress 2 or E.max ( new name for IPS Impress 2 ) .

Note : IPS empress 1 means leucite reinforced glass ceramic , while IPs empress 2 means lithium disilicate reinforced glass ceramics .

E.max is a new name for IPS empress 2 and it was so called because it provides strength and beauty at the same time .

** regarding flexural strength :

IPS empress 2 / Emax is 440 mpa Vs. 120 mpa for IPS Impress 1 , “ IPS empress 2 is  3 fold more than IPS empress 1 “ .

** IPs empress 1 can be used for Inlays , Onlays , veneers and crowns , E.max also have the same uses added to it a 3 unit anterior bridge .

Note : ( posteriorly they have a high fracture rate , so they are not used ) .

** the needle like structure crystals provided by the lithium in “ lithium disilicate ceramics “ , prevent the crack from propagation along the ceramic . ( As an answer to a question ) .

** Itching time when lithium disilicate is used is less than the itching time when feldspathic porcelain or leucite based ceramics are used. lithium disilicate require only 10 – 20% seconds ( depending on the concentration of the itchant ) while leucite based ceramics require 60 seconds and above .

** nowadays we use alumina and zirconia , but the Ceramis are not used anymore .

** In Zirconia , we use yttrium oxide partially stabilized tetragonal zirconia polycrystals .

** As we know ceramics are brittle , so there are strengthening mechanisms to overcome this problem , these mechanism include :

- lamination over the metal , over the tooth structure or over another stronger particle , such as zirconium .

- dispersion strengthening , by leucites .

- compression , the edge of lithium tangential disilicate are compressed , this will prevent crack propagation .

- transformation toughening “ when we have crystals in more than one configuration ( more than one type of crystals )

** In Zirconia , we have different crystals configurations , these include :

- Tetragonal poly crystals  these are available in high temperatures only

- Monoclinic crystals

- Cubic crystals

2. & 3.  are available in room temperature .

*** Tetragonal polycrystals have a smaller volume than monoclinic or cubic crystals and they are only available in high temperatures . To be able to stabilize these crystals at room temperature , we should add yttria OR calcia OR ceria ( yttrium oxide , calcium oxide or cerium oxide ).

** if these materials are added in a high percentage , we will have a total stabilization but we add them in small percentage .

EX. YTZP tetragonal polycrystals have 97% zirconia oxide and 2.5% mmol by volume yttrium oxide . In this case, the yttrium oxide provided partial stabilization , If we have total stabilization by adding yttrium oxide in a high percentage , this will be useless .

** we desire partial stabilization ; because when we have a high pressure load that may lead to a crack , the yttrium oxide will cause a change in the crystals shape from tetragonal to monoclinic polycrystals , the monoclinic polycrystals have larger shape and they will close the crack .

special thanks to Khaldon for helping me .

Nasma Atamleh & khaldon ALqaddumi